|  | Assessment Evidence Guide For 9. Auto Body & Paint Technician Level-4(Part-I) Formative Assessment 76. Apply Primer Surface |
| --- | --- |
|  | Date 15-19 September, 2020 Lahore |
|  | National Vocational & Technical Training Commission |

Instruction Sheet for the Candidate

| Qualification | Automobile Technology L-4 (P-I) (9. Auto Body & Paint Technician) |
| --- | --- |
| Competency Standard(s) | 76. Apply Primer Surface |
| Purpose of Assessment | Formative Assessment |

| Candidate Details | Name____________________________________________________ Registration/Roll Number_______________________________________________ |
| --- | --- |
| Guidance for Candidate | To meet this standard, you are required to complete the following within the given time frame (for practical demonstration & assessment) - Scuffing for primer Surface with sanding machine - Scuffing for primer Surface with hand sanding block - Cleaning & degreasing before primer Surface application - Masking before primer Surface application - Mixing of primer Surface - Primer Surface application - Drying of primer Surface From infrared heater |
| Time: 03 hrs. | During a practical assessment, under observation by an assessor, you are required to - Determine the areas for scuffing primer Surface - Determine the areas that need to be masking - Attached 320 grit sand paper with dual action sander - Scuff the surface to a distance of 100mm from the edge - Bring the sander into contact with the panel before starting the sander - Scuffing the act of finely scratching a surface with sandpaper - Clean the work place - Wear PPE according to instruction - Attached 320 grit sand paper with hand sanding block - Attached hand sanding blocks with dust extraction machine - Blow air on the surface to dry the degreaser - Protect all body for over spray use masking foil - Calculate the amount of primer to be Mixed - Mix it primer Surface& hardener according to manufacturer’s instructions - Pour the primer Surface in to the mixing container according to job - Mask the body that need to be protected - Strain the primer Surface using a strainer according to instruction - Pour the primer Surface in to the spray gun - Adjust the air pressure according to instruction - Adjust the spray gun - Apply primer Surface according to specified method - Clean the spray gun after work finish - Adjust the distance of infrared heater between panel - Adjust the timer of infrared heater according to standard |
| Minimum Evidence Required |  |

Self-Assessment Checklist

| Candidate Name |  |
| --- | --- |
| Registration No. |  |
| Qualification | Automobile Technology L-4 (P-I) (9. Auto Body & Paint Technician) |
| Competency Standards | 76. Apply Primer Surface |
| Assessment Task | 1. Scuffing for primer Surface with sanding machine 2. Scuffing for primer Surface with hand sanding block 3. Cleaning & degreasing before primer Surface application 4. Masking before primer Surface application 5. Mixing of primer Surface 6. Primer Surface application 7. Drying of primer Surface From infrared heater |

I can……………….

| Performance Criteria | Yes | No |
| --- | --- | --- |
| - Determine the areas for scuffing primer Surface |  |  |
| - Determine the areas that need to be masking |  |  |
| - Attached 320 grit sand paper with dual action sander |  |  |
| - Scuff the surface to a distance of 100mm from the edge |  |  |
| - Bring the sander into contact with the panel before starting the sander |  |  |
| - Scuffing the act of finely scratching a surface with sandpaper |  |  |
| - Clean the work place |  |  |
| - Wear PPE according to instruction |  |  |
| - Attached 320 grit sand paper with hand sanding block |  |  |
| - Attached hand sanding blocks with dust extraction machine |  |  |
| - Blow air on the surface to dry the degreaser |  |  |
| - Protect all body for over spray use masking foil |  |  |
| - Calculate the amount of primer to be Mixed |  |  |
| - Mix it primer Surface& hardener according to manufacturer’s instructions |  |  |
| - Pour the primer Surface in to the mixing container according to job |  |  |
| - Mask the body that need to be protected |  |  |
| - Strain the primer Surface using a strainer according to instruction |  |  |
| - Pour the primer Surface in to the spray gun |  |  |
| - Adjust the air pressure according to instruction |  |  |
| - Adjust the spray gun |  |  |
| - Apply primer Surface according to specified method |  |  |
| - Clean the spray gun after work finish |  |  |
| - Adjust the distance of infrared heater between panel |  |  |
| - Adjust the timer of infrared heater according to standard |  |  |

Candidate’s Signature___________________	Assessor’s Signature_____________________

Date: ________________________________

Assessors Judgment Guide

| Qualification | Automobile Technology L-4 (P-I) (9. Auto Body & Paint Technician) |
| --- | --- |
| Competency Standard(s) | 76. Apply Primer Surface |
| Candidate Details | Name: ____________________________________________________________________ Registration/Roll Number: ________________________Signature: ____________________ |
| Assessment Outcome | COMPETENT NOT YET COMPETENT Name of the Assessor ________________________Assessor’s code: ___________________ Signature: __________________________________ |

| Assessment Summary (to be filled by the assessor) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Activity | Method |  |  |  |  | Result |  |
| Nature of Activity | Written | Oral | Observation | Portfolio | Role Play | Competent | Not Yet Competent |
| Practical Skill Demonstration |  |  |  |  |  |  |  |
| Knowledge Assessment |  |  |  |  |  |  |  |
| Other Requirement |  |  |  |  |  |  |  |

Observation Checklist

| Assessment Task |  | - Scuffing for primer Surface with sanding machine - Scuffing for primer Surface with hand sanding block - Cleaning & degreasing before primer Surface application - Masking before primer Surface application - Mixing of primer Surface - Primer Surface application - Drying of primer Surface From infrared heater |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| During the practical assessment, candidate demonstrated the following: |  |  |  | Yes | No | Remarks |
|  | Determine the areas for scuffing primer Surface |  |  |  |  |  |
|  | Determine the areas that need to be masking |  |  |  |  |  |
|  | Attached 320 grit sand paper with dual action sander |  |  |  |  |  |
|  | Scuff the surface to a distance of 100mm from the edge |  |  |  |  |  |
|  | Bring the sander into contact with the panel before starting the sander |  |  |  |  |  |
|  | Scuffing the act of finely scratching a surface with sandpaper |  |  |  |  |  |
|  | Clean the work place |  |  |  |  |  |
|  | Wear PPE according to instruction |  |  |  |  |  |
|  | Attached 320 grit sand paper with hand sanding block |  |  |  |  |  |
|  | Attached hand sanding blocks with dust extraction machine |  |  |  |  |  |
|  | Blow air on the surface to dry the degreaser |  |  |  |  |  |
|  | Protect all body for over spray use masking foil |  |  |  |  |  |
|  | Calculate the amount of primer to be Mixed |  |  |  |  |  |
|  | Mix it primer Surface& hardener according to manufacturer’s instructions |  |  |  |  |  |
|  | Pour the primer Surface in to the mixing container according to job |  |  |  |  |  |
|  | Mask the body that need to be protected |  |  |  |  |  |
|  | Strain the primer Surface using a strainer according to instruction |  |  |  |  |  |
|  | Pour the primer Surface in to the spray gun |  |  |  |  |  |
|  | Adjust the air pressure according to instruction |  |  |  |  |  |
|  | Adjust the spray gun |  |  |  |  |  |
|  | Apply primer Surface according to specified method |  |  |  |  |  |
|  | Clean the spray gun after work finish |  |  |  |  |  |
|  | Adjust the distance of infrared heater between panel |  |  |  |  |  |
|  | Adjust the timer of infrared heater according to standard |  |  |  |  |  |
| Competent |  |  | Not Yet Competent |  |  |  |

Knowledge Assessment

| Qualification | Automobile Technology L-4 (P-I) (9. Auto Body & Paint Technician) |
| --- | --- |
| Competency Standard(s) | 76. Apply Primer Surface |
| Candidate Details | Name: _____________________________________________________________________ Registration/Roll Number: __________________ Candidate Signature: ________________ |
| Assessment Outcome | COMPETENT NOT YET COMPETENT Name of the Assessor: __________________________Assessor’s code: _________________ Signature of the Assessor: _______________________ |

Candidate’s response is not required to be identical, but similar concepts and/or keywords must be used. Oral questioning may be used to clarify candidate understanding of topic and its application.

| Questions (Candidate confidently answered questions correctly and demonstrated understanding of the topics and their application) |  | Satisfactory | Not Satisfactory |
| --- | --- | --- | --- |
|  | Write types of primers. |  |  |
|  | State about mixing of primer surfacer. |  |  |
|  | List instructions to be followed when using anticorrosive paints. |  |  |
|  | Primer-surfacer is often sprayed over body filler and the repair area to help level the repair area. - True. - False. |  |  |
|  | A primer-surfacer is a high-solids primer that fills small imperfections and usually must be sanded. - True. - False. |  |  |
|  | A plain _____ is a thin undercoat designed to provide good adhesion for the topcoat. |  |  |
|  | A primer-filler is a very _______ form of primer-surfacer. A. Thick B. Thick. |  |  |
| 8 | Which prime coat improves adhesion of the topcoat and seals old painted surfaces that have been sanded? A. Primer B. Primer-sealer C. Primer-filler D. Primer-surfacer |  |  |
| 9 | Define the terms prime coat and topcoat. |  |  |
| 10 | List instructions related to application of primer Surfacer |  |  |

Feedback to the Candidate

Candidate’s Signature _______________________Assessor’s Signature_________________________