Instruction Sheet for the Candidate

| Qualification | National Vocational Certificate Level-2 Glass & Ceramics (Supervisor) |
| --- | --- |
| Competency Standard(s) | Perform tableware manufacturing |
| Purpose of Assessment | Formative assessment |

| Candidate Details | Name ____________________________________________________________ Registration/Roll Number __________________________________________________ |
| --- | --- |
| Guidance for Candidate | To meet this standard, you are required to complete the following within the given time frame (for practical demonstration and assessment): - 50 kg Slip is provided to prepare the 1 no of complete green ware tea set by casting technique (2 hr ) - 500 kg of slip is provided to make 6 no of bowls and plate by jiggering and jollying process (3 hr ) |
| Time: 05 hr | During a practical assessment, under observation by an assessor, you are required to 50 kg Slip is provided to prepare the 1 no of complete green ware tea set by casting technique Perform Casting ofTable Ware Handle the slip. Check the density & viscosity of the slip. Identify the tools and equipment required during casting. Select the suitable moulds. Control the filling speed & position of the pored slip. Check cast thickness. Calculate the removing cast time. Handle the cast getting stucked in the mould. Identify the defects of the casting. Perform Finishing and Joining of Table Ware Identify the Green product as per specification Identify the Defects as per specification. check moisture content of green product identify the different cutting tools as per job requirement Cut the Scrap according to the mark Finish the Product as per requirement. Identify the Joining paste Apply the Paste to the joining parts Ensure Proper joining Remove extra clay from the article Finish Full body by using sponge and water as required Clean the Piece as per requirements Finalize the product .Perform drying of Table ware Check the green product to ensure desired condition Start the dryer as per operating procedure Check the Temperature as per job requirement Place the Product on the conveyer / round dryer as per specifications Unload dried product from the dryer as per procedure. Set the humidity & temperature of dryer if required. Check the moisture of the dried ware - 500 kg of slip is provided to make 6 no of bowls and plate by jiggering and jollying process Prepare the pug mill Check the vacuum of the pug mill Check the hardness of blank Cut the blank as per requirement Check the RPM of roller head and spindle Check the Temperature of roller head and spindle Adjust Roller head up and down level as per product specification Adjust the Edge cutter. Make the Machine ready to operate in accordance with work instructions Check the Mould Condition as per specification Prepare Mould as required Fix Mould on the spindle as per procedure Put Clay slice on the mould according to instruction Check clay slice to be pressed and formed Identify the Defects of the product Remove the product with mould |
| Minimum Evidence Required |  |

Self-Assessment Checklist

| Candidate Name |  |
| --- | --- |
| Registration No. |  |
| Qualification | National Vocational Certificate Level-2 Glass & Ceramics (Supervisor) |
| Competency Standards | Perform tableware manufacturing |
| Assessment Task | - 50 kg Slip is provided to prepare the 1 no of complete green ware tea set by casting technique (2 hr ) - 500 kg of slip is provided to make 6 no of bowls and plate by jiggering and jollying process (3 hr ) |

I can……………….

| Performance Criteria | Yes | No |
| --- | --- | --- |

Candidate’s Signature _______________	Assessor’s Signature _______________

Date: ____________________

Assessors Judgment Guide

| Qualification | National Vocational Certificate Level-2 Glass & Ceramics (Supervisor) |
| --- | --- |
| Competency Standard(s) | Perform tableware manufacturing |
| Candidate Details | Name: ____________________________________________________________ Registration/Roll Number: ____________________Signature: ____________________ |
| Assessment Outcome | COMPETENT NOT YETCOMPETENT Name of the Assessor ____________________ Assessor’s code: __________ Signature:____________________ |

| Assessment Summary (to be filled by the assessor) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Activity | Method |  |  |  |  | Result |  |
| Nature of Activity | Written | Oral | Observation | Portfolio | Role Play | Competent | Not Yet Competent |
| Practical Skill Demonstration |  |  |  |  |  |  |  |
| Knowledge Assessment |  |  |  |  |  |  |  |
| Other Requirement |  |  |  |  |  |  |  |

Observation Checklist

| Assessment Task |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| During the practical assessment, candidate demonstrated the following: |  |  |  | Yes | No | Remarks |
| Competent |  |  | Not Yet Competent |  |  |  |

Knowledge Assessment

| Qualification | National Vocational Certificate Level-2 Glass & Ceramics (Supervisor) |
| --- | --- |
| Competency Standard(s) | Perform tableware manufacturing |
| Candidate Details | Name: __________________________________________________ Registration/Roll Number: ____________________ Candidate Signature: __________ |
| Assessment Outcome | COMPETENT NOT YETCOMPETENT Name of the Assessor: ____________________Assessor’s code: ____________________ Signature of the Assessor: ____________________ |
| Candidate’s response is not required to be identical, but similar concepts and/or keywords must be used. Oral questioning may be used to clarify candidate understanding of topic and its application. |  |

| Questions (Candidate confidently answered questions correctly and demonstrated understanding of the topics and their application) |  | Satisfactory | Not Satisfactory |
| --- | --- | --- | --- |
|  | Describe the table ware body and transparent glaze recipe |  |  |
|  | Candidate’s response |  |  |
|  | Describe the table ware body and glaze faults |  |  |
|  | Describe the different types of moulds |  |  |
|  | Describe the dryer used in the table ware industry |  |  |
|  | Describe the defects of table ware fired body |  |  |

Feedback to the Candidate

Candidate’s Signature____________________Assessor’s Signature____________________