## Module: Prepare Moulds And Models

Objective: This module covers the knowledge and  skills required to Prepare draft Pattern for Model, Prepare Plaster / Resin Model, Prepare Plaster Mould, Perform Finishing of the Mould, Rectify defects in moulds and models, Inspect and store Moulds / Models

Duration:  150 Hours			Theory:  20 Hours		Practice:  130 Hours                  Credit Hours:  15

| Learning Unit | Learning Outcomes | Learning Elements | Duration | Materials Required | Learning Place |
| --- | --- | --- | --- | --- | --- |
| - Prepare draft Pattern for Model | Trainee will be able to: - Understand basic tools and mathematic calculation - Do Basic Drawing and Draft - Perform Tracing of Pattern | - Describe the functions of the tools used in pattern making. - Demonstrate the basic geometric shapes. - Demonstrate the process of tracing. Practical Activity: - Draw geometrical pattern of given model. | Theory- 2Hrs Practical- 20Hrs Total- 22Hrs | - Geometrical Tools - Tracing Papers - Tracing Pencils - T-Square - Set Square | Classroom Training Workshop Lab/ |
| - Prepare Plaster / Resin Model | Trainee will be able to: - Calculate Clay Body Shrinkage - Batching / Mixing of Plaster - Working on Modeling Wheel / Direct Carving / Lathe Machine / CNC Machine - Inspection of Final Model - Handle & store plaster properly - Calculate the setting time of plaster. | - Explain the quality of plaster of paris / resin. - Apply basic arithmetic calculation. - Make use of modelling wheel. - Identify setting time of plaster of paris. Practical Activity: - Develop Plaster model of given sample. | Theory- 2Hrs Practical- 10Hrs Total- 12Hrs | - Plaster of paris - Set of Cutting tools - Modelling wheel - Mixer - Vacuum pump - Geometric tools - T-Square - Set Square | Classroom Training Workshop Lab/ |
| - Prepare Plaster Mould | Trainee will be able to: - Identify the Types of Mould (Plaster/Resin) - Identify Parting Solution & Shellac - Prepare Master Mould - Prepare / Develop Father Mould - Develop / Prepare Work Mould - Develop / Jiggering Mould - Drying the Mould - Identify the faults in models. | - Explain the quality of plaster of paris / resin. - Apply basic arithmetic calculation. - Demonstrate the types of moulds. - Master Mould - Father / Case Mould - Working Mould - Jiggering Mould - Identify drying time of mould. - Demonstrate the faults in moulds. Practical Activity: - Develop Plaster mould of given model. | Theory- 4Hrs Practical- 40Hrs Total- 44Hrs | - Plaster of paris - Set of Cutting tools - Modelling wheel - Mixer - Vacuum pump - Geometric tools - T-Square - Set Square - Metallic / Resin Dies - Clamps - Plastic Bottons - Soap - Wax - Sprit - Sand Paper - Sponges - Brush | Classroom Training Workshop Lab/ Field Visit |
| - Perform Finishing of the Mould | Trainee will be able to: - Repair defects occurring during the moulding process - Remove inserts or loose pieces and replace in mould - Prepare the surface of the mould. - surface finishes - Cure or dry the mould in accordance with the specification | - Demonstrate the finishing process of moulds. Practical Activity: - Perform finishing of given mould. | Theory- 4Hrs Practical- 40Hrs Total- 44Hrs | - Plaster of paris - Set of Cutting tools - Modelling wheel - Mixer - Vacuum pump - Geometric tools - T-Square - Set Square - Metallic / Resin Dies - Clamps - Plastic Bottons - Soap - Wax - Sprit - Sand Paper - Sponges - Brush | Classroom Training Workshop Lab/ Field Visit |
| - Rectify defects in moulds and models | Trainee will be able to: - Identify the range of faults that can occur during the operation - Determine and rectify fault causes by /work instructions - Identify and rectify equipment failure causes in accordance with procedures/work instructions - Make sure appropriate records and log books of equipment - operations are maintained to meet procedures/work instructions - Identify non-routine problems and report to designated person. | - Demonstrate defects occurred in modelling / moulding. - Illustrate process of repairing the models / moulds. - Organize records and log book. Practical Activity: - Identify the defects in given moulds. | Theory- 4Hrs Practical- 10Hrs Total- 14Hrs | - Plaster of paris - Plaster Moulds - Spirit - Sand Paper - Sponges - Blades | Classroom Training Workshop Lab/ Field Visit |
| - Inspect and store Moulds / Models | Trainee will be able to: - Inspect moulds / model for defects - Store the Moulds and Model in accordance with specification and procedures/work instructions. | - Describe the inspection procedures for moulds / models. - Illustrate the storage procedure for moulds / models. Practical Activity: - Plan storage of given samples of moulds / models. | Theory- 4Hrs Practical- 10Hrs Total- 14Hrs | - Models - Moulds | Classroom Training Workshop Lab/ Field Visit |