## Module: Perform Tableware Manufacturing

Objective: This module covers the knowledge and  skills required to Perform Batching of Table ware Body, Perform Batching of Table ware Glaze, Perform Modelling & Mould making of Table ware, Perform Casting of Table Ware, Perform Jiggering of Table Ware, Perform Finishing and Joining of Table Ware, Perform drying of Table ware, Perform Glazing of Table ware, Perform Firing of Table wares, Perform Sorting & packing of Table wares

Duration:  270 Hours			Theory:  40 Hours		Practice:  230 Hours                  Credit Hours:  27

| Learning Unit | Learning Outcomes | Learning Elements | Duration | Materials Required | Learning Place |
| --- | --- | --- | --- | --- | --- |
| - Perform Batching of Table ware Body | Trainee will be able to: - Check the job card - Identify the raw materials - Check the moisture - operate the ball mills - Operate the de - dusting plant - Check residue, viscosity and Particle size analysis of the slip - Identify the body deflocculants. - Complete appropriate record and log | - Describe the body composition of table ware body - Enlist equipment’s used in slip house - Describe the working principle of processing equipments - Explain different quality control test involved in body preparation Practical Activity: Prepare the 50 kg batch of table ware body | Theory- 4Hrs Practical- 10Hrs Total- 14Hrs | Ball Mill Jaw Crusher Blunger Filter Press Magnatic separator Sieves Viscometer Hydrometer Weight Balance | Classroom Training Workshop Lab/ Field Visit |
| - Perform Batching of Table ware Glaze | Trainee will be able to: - Check the job card - Identify the raw materials - Check the moisture - operate the ball mills - Check residue, viscosity and Particle size analysis of the glaze. - Identify the glaze deflocculants. - Identify the glaze faults. - Identify the glaze stain. - Prepare the color glazes. - Complete appropriate record and log | - Describe the glaze composition of table ware body - Enlist equipment’s used in slip house - Describe the working principle of processing equipment - Explain different quality control test involved in glaze preparation Practical Activity: Prepare the 50 kg batch of table ware glaze | Theory- 4Hrs Practical- 20Hrs Total- 24Hrs | - Ball Mill - Jaw Crusher - Blunger - Filter Press - Magnatic separator - Sieves - Weight Balance | Classroom Training Workshop Lab/ Field Visit |
| - Perform Modelling & Mould making of Table ware | Trainee will be able to: - Check plaster quality for moulds - Identify the types of the material used e.g. Plaster of paris, resin. - Identify the tools for mould& model making. - Identify the material used as parting solution to seal the pores of mould. - Calculate the clay body shrinkage in respect of models | - Describe the model and different types of moulds - Explain the working of modelling wheel - Describe modelling tools - Describe the making of jiggering mould Practical Activity: Prepare the model of the large Vase | Theory- 4Hrs Practical- 40Hrs Total- 44Hrs | - Plaster of Paris - Modelling Wheel - Plaster tools - Shellec etc. | Classroom Training Workshop Lab/ Field Visit |
| - Perform Casting of Table Ware | Trainee will be able to: - Handle the slip. - Check the density & viscosity of the slip. - Identify the tools and equipment required during casting. - Select the suitable moulds. - Control the filling speed & position of the pored slip. - Check cast thickness. - Calculate the removing cast time. - Handle the cast getting stucked in the mould. - Identify the defects of the casting. - Operate battery casting, pressure casting machine. | - Describe the slip casting techniques - Understand casting defects - Illustrate casting process - Describe casting time and thickness Practical Activity: Perform the casting of the given Tea set | Theory- 4Hrs Practical- 20Hrs Total- 24Hrs | - Plaster Moulds of various sizes - Slip - Mixer - Hydrometer - Viscometer - Weight Balance | Classroom Training Workshop Lab/ Field Visit |
| - Perform Jiggering of Table Ware | Trainee will be able to: - Prepare the pug mill - Check the vacuum of the pug mill - Check the hardness of blank - Cut the blank as per requirement - Check the RPM of roller head and spindle - Check the Temperature of roller head and spindle - Adjust Roller head up and down level as per product specification - Adjust the Edge cutter. - Make the Machine ready to operate in accordance with work instructions - Check the Mould Condition as per specification - Prepare Mould as required - Fix Mould on the spindle as per procedure - Put Clay slice on the mould according to instruction - Check clay slice to be pressed and formed - Identify the Defects of the product - Remove the product with mould | Describe Jiggering and Jollying techniques Explain the working of the pug mill Explain the working of jiggering machine Describe the defects arise during jiggering Machine Practical Activity: Prepare the Cup and bowl with the help of jiggering machine | Theory- 2Hrs Practical- 20Hrs Total- 22Hrs | - Pug Mill - Cutter - Jiggering and Jolleying Machine - Balance | Classroom Training Workshop Lab/ Field Visit |
| - Perform Finishing and Joining of Table Ware | Trainee will be able to: - Identify the Green product as per specification - Identify the Defects as per specification. - check moisture content of green product - identify the different cutting tools as per job requirement - Cut the Scrap according to the mark - Finish the Product as per requirement. - Identify the Joining paste - Apply the Paste to the joining parts - Ensure Proper joining - Remove extra clay from the article - Finish Full body by using sponge and water as required - Clean the Piece as per requirements - Finalize the product | - Describe Green wares - Explain Joining paste - Enlist the causes and remedies of defects - Importance of moisture and drying during finishing and joining - Enlist finishing and joining tools Practical Activity: Perform the finishing and joining of the given Tea Sets | Theory- 4Hrs Practical- 20Hrs Total- 24Hrs | - Round Wheel - Cutters - Sponges - Joining Paste | Classroom Training Workshop Lab/ Field Visit |
| - Perform drying of Table ware | Trainee will be able to: - Check the green product to ensure desired condition - Start the dryer as per operating procedure - Check the Temperature as per job requirement - Place the Product on the conveyer / round dryer as per specifications - Unload dried product from the dryer as per procedure. - Set the humidity & temperature of dryer if required. - Check the moisture of the dried ware. - Identify the drying defects. - Maintain Records and log books of equipment operations. - Identify the Non-routine problems and report to the designated person. | - Explain drying process - Describe the working of dryer Conveyor /Round dryer Loading and unloading in dryer - Practical Activity: - Perform the drying of given green wares | Theory- 2Hrs Practical- 20Hrs Total- 22Hrs | Conveyor /Round dryer - Moisture Analyzer - Weighing Balance - Green wares | Classroom Training Workshop Lab/ Field Visit |
| - Perform Glazing of Table ware | Trainee will be able to: - Adjust the viscosity & density of the glaze. - Identify the glazing technique. - Set up glaze application equipment for operation - Apply glaze to produce the specified thickness - Recover excess or spilt glaze for treatment or recycling - Identify the glazing defects. - Apply glaze repair techniques to produce a properly finished product - Ensure all glaze faults are removed - Identify the range of faults that can occur during the operation - Identify and rectify equipment failure causes in accordance with procedures/work instructions - Complete appropriate record and log - Identify non-routine problems and report to designated person. - Use PPEs(Personal Protective Equipment) | Describe the glazing and it applications Explain different types of glazing equipment Describe glazing defects - Practical Activity: Perform glazing of the given sizes of green ware Vase | Theory- 6Hrs Practical- 30Hrs Total- 36Hrs | - Glazing Booth - Spray Gun - Compressor - Viscometer - Hydrometer - Sponges - Green wares - Different glazes | Classroom Training Workshop Lab/ Field Visit |
| - Perform Firing of Table wares | Trainee will be able to: - Identify the Kilns e.g. tunnel kiln, roller kiln, shuttle kiln etc. - Determine the firing requirements from the production program - Identify and set up the kiln cars or furniture - Determine kiln and kiln furniture e.g. slabs, pillars, kiln lining and burners etc are within specification. - Determine the firing equipment is safe to operate - Check for fuel feed obstructions and clear burner pathways. - Ensure products are set or stacked to specification - Determine correct stacking pattern of green wares - Ensure adequate space is allowed around each item - Use kiln space effectively - Determine kiln firing cycle - Monitor and record kiln car movement, or kiln contents - Monitor and adjust kiln heating equipment (elements or burners) - and record temperature gradient details - Complete appropriate record and log - Identify non-routine problems and report to designated person - Use PPEs(Personal Protective Equipment) | - Describe Kiln types - Describe firing schedules for different bodies - Explain types of kiln furniture - Illustrate different types of Insulations - Explain different parts of kiln - Understanding of kiln data recording techniques - Firing cycle of different ceramics ware - Describe types of kiln burners - Practical Activity: Program and fire the Gas fired Kiln | Theory- 6Hrs Practical- 20Hrs Total- 26Hrs | - Shuttle Kiln with complete accessories - Pyrometer - Kiln Furniture - Kiln Car - Data Recorders - Spare BURNERS | Classroom Training Workshop Lab/ Field Visit |
| - Perform Sorting & packing of Table wares | Trainee will be able to: - Identify the defects - understand the quality standards - understand the quality control tools. - Identify the suitable packing & stacking. - Use PPEs(Personal Protective Equipment) | Describe Kiln firing defects Illustrate quality control techniques Describe sorting and packing techniques - Practical Activity: Perform the sorting of given fired ceramic ware. | Theory- 2Hrs Practical- 10Hrs Total- 12Hrs | Fired ceramics ware | Classroom Training Workshop Lab/ Field Visit |