Instruction Sheet for the Candidate

| Qualification | National Vocational Certificate Level-4 in Civil Technology (Concrete Technology) |
| --- | --- |
| Purpose of Assessment | Summative Assessment – Concrete Technology |
| Candidate Details | Name_______________________________________________________ Registration Number_________________________________________________ |
| Guidance for Candidate | To meet this standard you are required to complete the following within 05 Hrs. time frame (for practical demonstration & assessment): - Perform the Destructive and Non Destructive Tests on Hardened Concrete. - Knowledge Assessment |
| Time: 05 Hrs | During a practical assessment, under observation by an assessor, you are required to “Check the basic properties of concrete like compressive strength, modules of rupture and Flexural strength by destructive test and also perform the non destructive test“ demonstrating the following criteria: |
| Minimum Evidence Required | - Measure the cement and sand by weight and mix material thoroughly. - Test the prepared samples of 3,7,14, and 28 days - Record readings and plot graph for compressive strength - Check the sample of concrete beam as per specification - Place the specimen on loading points. - Measure the cross section of the tested specimen at each end and at center to calculate average depth and height. - Calculate Flexural strength by using formula. - Check the sample of concrete cylinder as per specifications. - Place the specimen on compression testing machine with complete arrangement. - Apply the continuous load within the range of 0.72 to 1.4 Mpa / Min. - Record the Flexural strength. - Calibrate rebound hammer and push hammer on surface. - Release the hammer and record the rebound number. - Find the compressive strength from graph. - Identify the apparatus for Rebar Detector test - Operate the instrument on required surface. - Detect the steel, its spacing and position |

Self-Assessment Checklist

| Candidate Name |  |
| --- | --- |
| Registration No. |  |
| Qualification | National Vocational Certificate Level-4 in Civil Technology (Concrete Technology) |
| Purpose of Assessment | Summative Assessment – Concrete Technology |
| Assessment Task | - Perform the Destructive and Non Destructive Tests on Hardened Concrete. |

I can……………….

| Performance Criteria | Yes | No |
| --- | --- | --- |
| - Measure the cement and sand by weight and mix material thoroughly. |  |  |
| - Test the prepared samples of 3,7,14, and 28 days |  |  |
| - Record readings and plot graph for compressive strength |  |  |
| - Check the sample of concrete beam as per specification |  |  |
| - Place the specimen on loading points. |  |  |
| - Measure the cross section of the tested specimen at each end and at center to calculate average depth and height. |  |  |
| - Calculate Flexural strength by using formula. |  |  |
| - Check the sample of concrete cylinder as per specifications. |  |  |
| - Place the specimen on compression testing machine with complete arrangement. |  |  |
| - Apply the continuous load within the range of 0.72 to 1.4 Mpa / Min. |  |  |
| - Record the Flexural strength. |  |  |
| - Calibrate rebound hammer and push hammer on surface. |  |  |
| - Release the hammer and record the rebound number. |  |  |
| - Find the compressive strength from graph. |  |  |
| - Identify the apparatus for Rebar Detector test |  |  |
| - Operate the instrument on required surface. |  |  |
| - Detect the steel, its spacing and position |  |  |

Candidate’s Signature__________________ Assessor’s Signature__________________

Date: _______________________________

Assessors Judgment Guide

| Qualification | National Vocational Certificate Level-4 in Civil Technology (Concrete Technology) |
| --- | --- |
| Purpose of Assessment | Summative Assessment – Concrete Technology |
| Candidate Details | Name:______________________________________________________________ Registration Number: ________________________Signature: _________________ |
| Assessment Outcome | COMPETENT NOT YETCOMPETENT Name of the Assessor________________________________________________ Assessor’s code:___________________Signature:________________________ |

| Assessment Summary (to be filled by the assessor) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Activity | Method |  |  |  |  | Result |  |
| Nature of Activity | Written | Oral | Observation | Portfolio | Role Play | Competent | Not Yet Competent |
| Practical Skill Demonstration |  |  |  |  |  |  |  |
| Knowledge Assessment |  |  |  |  |  |  |  |
| Other Requirement |  |  |  |  |  |  |  |

Observation Checklist

| Assessment Task |  | - Perform the Destructive and Non Destructive Tests on Hardened Concrete. |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| During the practical assessment, candidate demonstrated the following: |  |  |  | Yes | No | Remarks |
|  | Measure the cement and sand by weight and mix material thoroughly. |  |  |  |  |  |
|  | Test the prepared samples of 3,7,14, and 28 days |  |  |  |  |  |
|  | Record readings and plot graph for compressive strength |  |  |  |  |  |
|  | Check the sample of concrete beam as per specification |  |  |  |  |  |
|  | Place the specimen on loading points. |  |  |  |  |  |
|  | Measure the cross section of the tested specimen at each end and at center to calculate average depth and height. |  |  |  |  |  |
|  | Calculate Flexural strength by using formula. |  |  |  |  |  |
|  | Check the sample of concrete cylinder as per specifications. |  |  |  |  |  |
|  | Place the specimen on compression testing machine with complete arrangement. |  |  |  |  |  |
|  | Apply the continuous load within the range of 0.72 to 1.4 Mpa / Min. |  |  |  |  |  |
|  | Record the Flexural strength. |  |  |  |  |  |
|  | Calibrate rebound hammer and push hammer on surface. |  |  |  |  |  |
|  | Release the hammer and record the rebound number. |  |  |  |  |  |
|  | Find the compressive strength from graph. |  |  |  |  |  |
|  | Identify the apparatus for Rebar Detector test |  |  |  |  |  |
|  | Operate the instrument on required surface. |  |  |  |  |  |
|  | Detect the steel, its spacing and position |  |  |  |  |  |
| Competent |  |  | Not Yet Competent |  |  |  |

Knowledge Assessment

| Qualification | National Vocational Certificate Level-4 in Civil Technology (Concrete Technology) |
| --- | --- |
| Purpose of Assessment | Summative Assessment – Concrete Technology |
| Candidate Details | Name:______________________________________________________________ Registration Number: __________________ Candidate Signature:_____________ |
| Assessment Outcome | COMPETENT NOT YET COMPETENT Name of the Assessor:__________________________ Assessor’s code:_________________Signature of the Assessor:_______________ |

Candidate’s response is not required to be identical, but similar concepts and/or keywords must be used. Oral questioning may be used to clarify candidate understanding of topic and its application.

| Questions (Candidate confidently answered questions correctly and demonstrated understanding of the topics and their application) |  | Satisfactory | Not Satisfactory |
| --- | --- | --- | --- |
|  | In which unit the concrete has been measured. |  |  |
|  | What is meant by High Strength concrete |  |  |
|  | How much percentage of concrete strength has been gain upto 7 days with respect to 28 days strength |  |  |
|  | Up to how much days curing of concrete should be done. |  |  |
|  | As a rough estimate, we take ------- % of compressive strength as the MOR. |  |  |
|  | Which types of properties of structural material are provided by Non destructive testing. |  |  |
|  | What is the main advantage of using Non Destructive testing. |  |  |
|  | Which non destructive test is used to find the spacing of steel bar in structure. |  |  |

Feedback to the Candidate

Candidate’s Signature__________________Assessor’s Signature ___________________