Instruction Sheet for the Candidate

| Qualification | Level-5 Mechanical Technology (Foundry & Casting) |
| --- | --- |
| Competency Standard | Perform Foundry Work |
| Purpose of Assessment | Formative Assessment – Preform Foundry Work |
| Candidate Details | Name_______________________________________________________ Registration Number_________________________________________________ |
| Guidance for Candidate | To meet this standard you are required to complete the following within 04 Hrs. time frame (for practical demonstration & assessment): - Cast Journal Bearing Body - Practice casting through shell molding |
| Time: 04 Hrs. | During a practical assessment, under observation by an assessor, you are required to “Perform Foundry Work, Cast through sand moulding of Journal Bearing Body and Casting through shell moulding as per Annexure-A “ demonstrating the following criteria: |
| Minimum Evidence Required | 1-Cast Journal Bearing Body - Prepare green sand. Place the drag on Moulding Board and fix the split pattern of journal bearing in the drag as per drawing. - Transfer sand and perform ramming operation. - Remove excessive sand from drag with the help of strike of bar. Flip the drag and sprinkle parting sand. - Fix the cope on drag and place runner, adjust sprue pin and riser accordingly - Fill cope with green sand and rammed the sand. Remove excessive sand from cope. - Perform venting as per standard and Produce pouring basin. - Split up cope and drag and make gating system. Carefully extract pattern and repair Mould cavities. - Preheat the mould to remove moisture content before pouring. - Melt metal to be pour in crucible. Dross out slag by adding slag coagulants with the help of skimmer. - Pour molten metal into the mould from crucible and let it cool. 2-Casting through shell molding - Prepare sand mixed thermosetting binder and fill the mould. - Firmly clamp heated match plate pattern on the molding box. Invert or roll over the mold box containing sand mixed with thermosetting material. - Reposition the moulding box so that all loose sand fell down and form a hard shell after curing. - Heat sand shell for a few minutes in oven for the purpose of complete curing. - Stripped shell mould from the pattern. - Assemble or match two halves of the shell mould and support them by metal shots and pouring sand into a box. - Pour molten metal into the cavity. |

Self-Assessment Checklist

| Candidate Name |  |
| --- | --- |
| Registration No. |  |
| Qualification | Level-5 Mechanical Technology (Foundry & Casting) |
| Competency Standards | Perform Foundry Work |
| Purpose of Assessment | Formative Assessment – Preform Foundry Work |
| Assessment Task | - Cast Journal Bearing Body - Practice casting through shell molding |

I can……………….

| Performance Criteria | Yes | No |
| --- | --- | --- |
| 1-Cast Journal Bearing Body |  |  |
| - Prepare green sand. Place the drag on Moulding Board and fix the split pattern of journal bearing in the drag as per drawing. |  |  |
| - Transfer sand and perform ramming operation. |  |  |
| - Remove excessive sand from drag with the help of strike of bar. Flip the drag and sprinkle parting sand. |  |  |
| - Fix the cope on drag and place runner, adjust sprue pin and riser accordingly |  |  |
| - Fill cope with green sand and rammed the sand. Remove excessive sand from cope. |  |  |
| - Perform venting as per standard and Produce pouring basin. |  |  |
| - Split up cope and drag and make gating system. Carefully extract pattern and repair Mould cavities. |  |  |
| - Preheat the mould to remove moisture content before pouring. |  |  |
| - Melt metal to be pour in crucible. Dross out slag by adding slag coagulants with the help of skimmer. |  |  |
| - Pour molten metal into the mould from crucible and let it cool. |  |  |
| 2-Casting through shell molding |  |  |
| - Prepare sand mixed thermosetting binder and fill the mould. |  |  |
| - Firmly clamp heated match plate pattern on the molding box. Invert or roll over the mold box containing sand mixed with thermosetting material. |  |  |
| - Reposition the moulding box so that all loose sand fell down and form a hard shell after curing. |  |  |
| - Heat sand shell for a few minutes in oven for the purpose of complete curing. |  |  |
| - Stripped shell mould from the pattern. |  |  |
| - Assemble or match two halves of the shell mould and support them by metal shots and pouring sand into a box. |  |  |
| - Pour molten metal into the cavity. |  |  |

Candidate’s Signature__________________ Assessor’s Signature__________________

Date: _______________________________

ANNUXURE-A

Assessors Judgment Guide

| Qualification | Level-5 Mechanical Technology (Foundry & Casting) |
| --- | --- |
| Competency Standards | Perform Foundry Work |
| Purpose of Assessment | Formative Assessment – Preform Foundry Work |
| Candidate Details | Name:______________________________________________________________ Registration Number: ________________________ Signature: _________________ |
| Assessment Outcome | COMPETENT NOT YET COMPETENT Name of the Assessor________________________________________________ Assessor’s code:___________________ Signature:________________________ |

| Assessment Summary (to be filled by the assessor) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Activity | Method |  |  |  |  | Result |  |
| Nature of Activity | Written | Oral | Observation | Portfolio | Role Play | Competent | Not Yet Competent |
| Practical Skill Demonstration |  |  |  |  |  |  |  |
| Knowledge Assessment |  |  |  |  |  |  |  |
| Other Requirement |  |  |  |  |  |  |  |

Observation Checklist

| Assessment Task |  | - Cast Journal Bearing Body - Practice casting through shell molding |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| During the practical assessment, candidate demonstrated the following: |  |  |  | Yes | No | Remarks |
| 1-Cast Journal Bearing Body |  |  |  |  |  |  |
|  | Prepare green sand. Place the drag on Moulding Board and fix the split pattern of journal bearing in the drag as per drawing. |  |  |  |  |  |
|  | Transfer sand and perform ramming operation. |  |  |  |  |  |
|  | Remove excessive sand from drag with the help of strike of bar. Flip the drag and sprinkle parting sand. |  |  |  |  |  |
|  | Fix the cope on drag and place runner, adjust sprue pin and riser accordingly |  |  |  |  |  |
|  | Fill cope with green sand and rammed the sand. Remove excessive sand from cope. |  |  |  |  |  |
|  | Perform venting as per standard and Produce pouring basin. |  |  |  |  |  |
|  | Split up cope and drag and make gating system. Carefully extract pattern and repair Mould cavities. |  |  |  |  |  |
|  | Preheat the mould to remove moisture content before pouring. |  |  |  |  |  |
|  | Melt metal to be pour in crucible. Dross out slag by adding slag coagulants with the help of skimmer. |  |  |  |  |  |
|  | Pour molten metal into the mould from crucible and let it cool. |  |  |  |  |  |
| 2-Casting through shell molding |  |  |  |  |  |  |
|  | Prepare sand mixed thermosetting binder and fill the mould. |  |  |  |  |  |
|  | Firmly clamp heated match plate pattern on the molding box. Invert or roll over the mold box containing sand mixed with thermosetting material. |  |  |  |  |  |
|  | Reposition the moulding box so that all loose sand fell down and form a hard shell after curing. |  |  |  |  |  |
|  | Heat sand shell for a few minutes in oven for the purpose of complete curing. |  |  |  |  |  |
|  | Stripped shell mould from the pattern. |  |  |  |  |  |
|  | Assemble or match two halves of the shell mould and support them by metal shots and pouring sand into a box. |  |  |  |  |  |
|  | Pour molten metal into the cavity. |  |  |  |  |  |
| Competent |  |  | Not Yet Competent |  |  |  |

Candidate’s response is not required to be identical, but similar concepts and/or keywords must be used. Oral questioning may be used to clarify candidate understanding of topic and its application.

Knowledge Assessment

| Qualification | Level-5 Mechanical Technology (Foundry & Casting) |
| --- | --- |
| Competency Standards | Perform Foundry Work |
| Purpose of Assessment | Formative Assessment – Preform Foundry Work |
| Candidate Details | Name:______________________________________________________________ Registration Number: __________________ Candidate Signature:_____________ |
| Assessment Outcome | COMPETENT NOT YET COMPETENT Name of the Assessor:__________________________ Assessor’s code:_________________ Signature of the Assessor:_______________ |

| Questions (Candidate confidently answered questions correctly and demonstrated understanding of the topics and their application) |  | Satisfactory | Not Satisfactory |
| --- | --- | --- | --- |
|  | Question Name types of sand used according to casting? |  |  |
|  | Candidate’s response |  |  |
|  | Question Describe different types of moulding? |  |  |
|  | Candidate’s response |  |  |
|  | Question Define ramming, venting and gating? |  |  |
|  | Candidate’s response |  |  |
|  | Question What are casting processes? |  |  |
|  | Candidate’s response |  |  |
|  | Question Describe types of binders? |  |  |
|  | Candidate’s response |  |  |
|  | Question Advantages and disadvantages of shell moulding? |  |  |
|  | Candidate’s response |  |  |
| 7. | Question Describe Slag coagulants and their types? |  |  |
|  | Candidate’s response |  |  |

Feedback to the Candidate

Candidate’s Signature__________________ Assessor’s Signature ___________________