|  | Assessment Evidence Guide For Jewellery Electroplater Formative Assessment Perform Pre-Treatment of Jewellery Article |
| --- | --- |
|  | Date 19th to 23rd Aug, 2024 Lahore |
|  | National Vocational & Technical Training Commission |

Instruction Sheet for the Candidate

| Qualification | Jewelry Electroplater |
| --- | --- |
| Competency Standard | Perform Pre-Treatment of Jewellery Article |
| Purpose of Assessment | Formative Assessment |
| Candidate Details | Name______________________________________________________ Registration/Roll Number_______________________________________ |
| Guidance for Candidate | To meet this standard, you are required to complete the following within 2 Hrs. time frame (for practical demonstration & assessment): - Assess surface quality of jewelry article and prepare for pre-treatment. - Perform steam cleaning to provided jewelry article(s). - Perform Ultrasonic cleaning of jewelry article(s). - Perform Acid/Alkali cleaning of jewelry article(s). - Perform electrolytic cleaning of jewelry article(s). - Perform acid surface activation of the jewelry article(s). - Perform electroless plating on the jewelry article(s). |
| Time: 2 hrs. | During a practical assessment, under observation by an assessor, you are required to |
| Minimum Evidence Required | Assess surface quality of jewelry article and prepare for pre-treatment: - Check for any surface defects including marks, scratches and roughness. - Segregate Jewelry articles according to quality. - Perform deburring and/or buffing to polish surface of Jewelry article. - Inspect for faulty hinges and soldered joints. - Fix loose stones - Degrease article after buffing/polishing with a decreasing media (e.g. acetone, white spirit, trichloroethylene etc.) Perform steam cleaning - Setup steamer for cleaning process. - Clean Jewelry article with steam ensuring the article is free of any deposits (e.g. shellac, etc.). Perform Ultrasonic cleaning - Prepare solution for ultrasonic cleaning. - Adjust temperature and frequency parameters. - Degrease article after buffing/polishing with a decreasing media (e.g. acetone, white spirit, trichloroethylene etc.) - Fix the article in jig and clean Jewelry article using ultrasonic machine for required time - Rinse article with water to remove cleaning media. - Inspect cleaned surface of the article. Perform Acid/Alkali cleaning - Prepare recipe of the acid/alkali cleaning solution as per Jewelry metal. - Mix ingredients to make acidic/alkaline solution for cleaning. - Label solution container to mention the ingredients and hazards of the solution. - Fix the article in jig and clean Jewelry article using acidic/alkaline cleaning bath for required time. - Rinse article with distilled water to remove cleaning media. Perform electrolytic cleaning - Prepare electrolytic cleaning solution as per recipe. - Connect Jewelry article with electrode in electrolytic cleaning apparatus. - Adjust electric current and voltage parameters. - Clean article for required time. - Rinse article with distilled water to remove cleaning media. Perform acid surface activation - Prepare recipe of the acidic activation solution as per Jewelry metal. - Mix ingredients to make acid solution for activation. - Label solution container to mention the ingredients and hazards of the solution. - Fix the article in jig and activate Jewelry article using activation bath for the required time. - Rinse article with distilled water to remove activation media. Perform electroless plating - Prepare recipe of the electroless plating solution as per Jewelry metal. - Mix ingredients to make electroless solution for plating. - Label solution container to mention the ingredients and hazards of the solution. - Fix the article in jig and perform electroless plating of Jewelry article as per requirement. - Rinse article with distilled water to remove cleaning media |

Self-Assessment Checklist

| Candidate Name |  |
| --- | --- |
| Registration No. |  |
| Qualification | Jewelry Electroplater |
| Competency Standard | Perform Pre-Electroplating Activities |
| Purpose of Assessment | Formative Assessment |
| Assessment Task | - Assess surface quality of jewelry article and prepare for pre-treatment. - Perform steam cleaning to provided jewelry article(s). - Perform Ultrasonic cleaning of jewelry article(s). - Perform Acid/Alkali cleaning of jewelry article(s). - Perform electrolytic cleaning of jewelry article(s). - Perform acid surface activation of the jewelry article(s). - Perform electroless plating on the jewelry article(s). |

I can……………….

| Performance Criteria | Yes | No |
| --- | --- | --- |
| - Check for any surface defects including marks, scratches and roughness. |  |  |
| - Segregate Jewelry articles according to quality. |  |  |
| - Perform deburring and/or buffing to polish the surface of the Jewelry article. |  |  |
| - Inspect for faulty hinges and soldered joints. |  |  |
| - Fix the loose stones |  |  |
| - Degrease article after buffing/polishing with a decreasing media (e.g. acetone, white spirit, trichloroethylene etc.) |  |  |
| - Assess the article if it needs steam cleaning treatment. |  |  |
| - If yes, setup steamer for cleaning process. |  |  |
| - Clean Jewelry article with steam ensuring the article is free of any deposits (e.g. shellac, etc.). |  |  |
| - Prepare solution for ultrasonic cleaning. |  |  |
| - Adjust temperature and frequency parameters. |  |  |
| - Degrease article after buffing/polishing with a decreasing media (e.g. acetone, white spirit, trichloroethylene etc.) |  |  |
| - Fix the article in jig and clean Jewelry article using ultrasonic machine for required time |  |  |
| - Rinse article with water to remove cleaning media. |  |  |
| - Inspect cleaned surface of the article. |  |  |
| - Prepare solution for ultrasonic cleaning. |  |  |
| - Prepare recipe of the acid/alkali cleaning solution as per Jewelry metal. |  |  |
| - Mix ingredients to make acidic/alkaline solution for cleaning. |  |  |
| - Label solution container to mention the ingredients and hazards of the solution. |  |  |
| - Fix the article in jig and clean Jewelry article using acidic/alkaline cleaning bath for required time. |  |  |
| - Rinse article with distilled water to remove cleaning media. |  |  |
| - Prepare electrolytic cleaning solution as per recipe. |  |  |
| - Connect Jewelry article with electrode in electrolytic cleaning apparatus. |  |  |
| - Adjust electric current and voltage parameters. |  |  |
| - Clean article for required time. |  |  |
| - Rinse article with distilled water to remove cleaning media. |  |  |
| - Assess the article if it needs acid surface activation. |  |  |
| - Prepare recipe of the acidic activation solution as per Jewelry metal. |  |  |
| - Mix ingredients to make acid solution for activation. |  |  |
| - Label solution container to mention the ingredients and hazards of the solution. |  |  |
| - Fix the article in jig and activate Jewelry article using activation bath for the required time. |  |  |
| - Rinse article with distilled water to remove activation media. |  |  |
| - Assess the article if it needs electroless plating prior to electroplating. |  |  |
| - Prepare recipe of the electroless plating solution as per Jewelry metal. |  |  |
| - Mix ingredients to make electroless solution for plating. |  |  |
| - Label solution container to mention the ingredients and hazards of the solution. |  |  |
| - Fix the article in jig and perform electroless plating of Jewelry article as per requirement. |  |  |
| - Rinse article with distilled water to remove cleaning media |  |  |

Candidate’s Signature__________________ Assessor’s Signature____________________

Date: _______________________________

Assessors Judgment Guide

| Qualification | Jewelry Electroplater |
| --- | --- |
| Competency Standard | Perform Pre-Electroplating Activities |
| Purpose of Assessment | Formative Assessment |
| Candidate Details | Name: ______________________________________________________________ Registration/Roll Number: ______________________ Signature: _______________ |
| Assessment Outcome | COMPETENT NOT YET COMPETENT Name of the Assessor________________________________________________ Assessor’s code: ____________________________________________________ Signature: ________________________________ |

| Assessment Summary (to be filled by the assessor) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Activity | Method |  |  |  |  | Result |  |
| Nature of Activity | Written | Oral | Observation | Portfolio | Role Play | Competent | Not Yet Competent |
| Practical Skill Demonstration |  |  |  |  |  |  |  |
| Knowledge Assessment |  |  |  |  |  |  |  |
| Other Requirement |  |  |  |  |  |  |  |

Observation Checklist

| Assessment Task |  | - Assess surface quality of jewelry article and prepare for pre-treatment. - Perform steam cleaning to provided jewelry article(s). - Perform Ultrasonic cleaning of jewelry article(s). - Perform Acid/Alkali cleaning of jewelry article(s). - Perform electrolytic cleaning of jewelry article(s). - Perform acid surface activation of the jewelry article(s). - Perform electroless plating on the jewelry article(s). |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| During the practical assessment, candidate demonstrated the following: |  |  |  | Yes | No | Remarks |
|  | Check for any surface defects including marks, scratches and roughness. |  |  |  |  |  |
|  | Segregate Jewelry articles according to quality. |  |  |  |  |  |
|  | Perform deburring and/or buffing to polish the surface of the Jewelry article. |  |  |  |  |  |
|  | Inspect for faulty hinges and soldered joints. |  |  |  |  |  |
|  | Fix the loose stones, if any. |  |  |  |  |  |
|  | Degrease article after buffing/polishing with a decreasing media (e.g. acetone, white spirit, trichloroethylene etc.) |  |  |  |  |  |
|  | Assess the article if it needs steam cleaning treatment. |  |  |  |  |  |
|  | If yes, setup steamer for cleaning process. |  |  |  |  |  |
|  | Clean Jewelry article with steam ensuring the article is free of any deposits (e.g. shellac, etc.). |  |  |  |  |  |
|  | Prepare solution for ultrasonic cleaning. |  |  |  |  |  |
|  | Adjust temperature and frequency parameters. |  |  |  |  |  |
|  | Degrease article after buffing/polishing with a decreasing media (e.g. acetone, white spirit, trichloroethylene etc.) |  |  |  |  |  |
|  | Fix the article in jig and clean Jewelry article using ultrasonic machine for required time |  |  |  |  |  |
|  | Rinse article with water to remove cleaning media. |  |  |  |  |  |
|  | Inspect cleaned surface of the article. |  |  |  |  |  |
|  | Prepare solution for ultrasonic cleaning. |  |  |  |  |  |
|  | Prepare recipe of the acid/alkali cleaning solution as per Jewelry metal. |  |  |  |  |  |
|  | Mix ingredients to make acidic/alkaline solution for cleaning. |  |  |  |  |  |
|  | Label solution container to mention the ingredients and hazards of the solution. |  |  |  |  |  |
|  | Fix the article in jig and clean Jewelry article using acidic/alkaline cleaning bath for required time. |  |  |  |  |  |
|  | Rinse article with distilled water to remove cleaning media. |  |  |  |  |  |
|  | Prepare electrolytic cleaning solution as per recipe. |  |  |  |  |  |
|  | Connect Jewelry article with electrode in electrolytic cleaning apparatus. |  |  |  |  |  |
|  | Adjust electric current and voltage parameters. |  |  |  |  |  |
|  | Clean article for required time. |  |  |  |  |  |
|  | Rinse article with distilled water to remove cleaning media. |  |  |  |  |  |
|  | Assess the article if it needs acid surface activation. |  |  |  |  |  |
|  | Prepare recipe of the acidic activation solution as per Jewelry metal. |  |  |  |  |  |
|  | Mix ingredients to make acid solution for activation. |  |  |  |  |  |
|  | Label solution container to mention the ingredients and hazards of the solution. |  |  |  |  |  |
|  | Fix the article in jig and activate Jewelry article using activation bath for the required time. |  |  |  |  |  |
|  | Rinse article with distilled water to remove activation media. |  |  |  |  |  |
|  | Assess the article if it needs electroless plating prior to electroplating. |  |  |  |  |  |
|  | Prepare recipe of the electroless plating solution as per Jewelry metal. |  |  |  |  |  |
|  | Mix ingredients to make electroless solution for plating. |  |  |  |  |  |
|  | Label solution container to mention the ingredients and hazards of the solution. |  |  |  |  |  |
|  | Fix the article in jig and perform electroless plating of Jewelry article as per requirement. |  |  |  |  |  |
|  | Rinse article with distilled water to remove cleaning media |  |  |  |  |  |
| Competent |  |  | Not Yet Competent |  |  |  |

Knowledge Assessment

| Qualification | Jewelry Electroplater |
| --- | --- |
| Competency Standard | Perform Pre-Electroplating Activities |
| Purpose of Assessment | Formative Assessment |
| Candidate Details | Name: ______________________________________________________________ Registration/Roll Number: _________________ Candidate Signature: ___________ |
| Assessment Outcome | COMPETENT NOT YET COMPETENT Name of the Assessor: ________________________________________________ Assessor’s code: ____________________________________________________ Signature of the Assessor: _______________________ |

Candidate’s response is not required to be identical, but similar concepts and/or keywords must be used. Oral questioning may be used to clarify candidate understanding of topic and its application.

| Questions (Candidate confidently answered questions correctly and demonstrated understanding of the topics and their application) |  | Satisfactory | Not Satisfactory |
| --- | --- | --- | --- |
|  | What is the primary purpose of pre-treatment in the electroplating process for jewelry articles? |  |  |
|  | What is steam cleaning in Jewellery articles? |  |  |
|  | What types of contaminants are typically removed during acid/alkali cleaning in the pre-treatment process? |  |  |
|  | What is process of electrolytic cleaning? |  |  |
|  | What challenges can arise if surface defects such as scratches are not addressed before electroplating? |  |  |
|  | How does electroless base coating differ from electroplating, and when is it applied in the pre-treatment process? |  |  |
|  | What role does pH control play in the acid/alkali cleaning process? |  |  |

Feedback to the Candidate

Candidate’s Signature__________________ Assessor’s Signature _________________

Answer Key

| What is the primary purpose of pre-treatment in the electroplating process for jewelry articles? | To remove contaminants, smoothen the surface, and ensure that the jewelry article is properly prepared for a high-quality electroplated finish. |
| --- | --- |
| What is steam cleaning in Jewellery articles? | It is pre-treatment of jewelry articles. In this procedure high-pressure steam remove dirt, oils, and other surface contaminants from jewelry articles, providing a clean surface for further processing. |
| What types of contaminants are typically removed during acid/alkali cleaning in the pre-treatment process? | Oxides, scales, rust, and organic residues |
| What is process of electrolytic cleaning? | Electrolytic cleaning involves passing an electric current through a solution to remove surface contaminants, offering a more controlled and effective cleaning method |
| What challenges can arise if surface defects such as scratches are not addressed before electroplating? | Surface defects can lead to poor adhesion of the electroplated layer, resulting in peeling, uneven thickness, and reduced durability. |
| How does electroless base coating differ from electroplating, and when is it applied in the pre-treatment process? | Electroless base coating is a chemical deposition process that does not require an external electric current, often used to apply a uniform base layer on complex shapes or as an undercoat for further electroplating. |
| What role does pH control play in the acid/alkali cleaning process? | pH control ensures that cleaning solution remains effective in dissolving contaminants without damaging the jewelry article or creating hazardous by-products. |