Course / Subject Name NQ-Mech-246. Workshop Practice-II (B) Perform Foundry and Casting

- MCQs

| Formative Assessment (Part A) | Formative Assessment (Part B) | Formative Assessment (Part C) |
| --- | --- | --- |
| LU 1 | LU 2-3 | LU 4-5 |
| - Controlling the moisture content of molding sand is important to : - Reduce the cost of the sand - Maintain mold strength and prevent defects - Improve the thermal conductivity of the sand - Enhance the surface finish of castings - Istrument used to measure the moisture content of molding sand is: - Pyrometer - Sand moisture tester - Permeability meter - Clay content tester - Excess moisture in molding sand can cause: - Blowholes - Shrinkage - Hot tears - Flash - The recommended range for moisture content in green sand is typically: - 0–2% - 2–8% - 10–15% - Above 20% - The clay content test in molding sand is performed to determine: - The sand’s permeability - The binder content of the sand - The sand’s chemical composition - The moisture absorption capacity - The clay content in molding sand is determined by: - Washing the sand and measuring sedimentation - Heating the sand to measure weight loss - Testing the thermal expansion of the sand - Compressing the sand to test its strength - What is the typical range of clay content in green molding sand? - 0–5% - 5–15% - 15–30% - 40–50% - The permeability test measures: - The sand's ability to retain its shape under stress - The flow of gases through the sand mold - The sand’s thermal expansion - The clay content of the sand - Green compressive strength refers to: - The sand’s ability to resist deformation when dry - The strength of molding sand with moisture present - The thermal strength of the sand - The sand’s resistance to gas flow - Which instrument is used to measure green compressive strength? - Permeability meter - Universal sand strength tester - Sand moisture tester - Sieve analysis machine - What does the fineness number of sand represent? - The thermal conductivity of the sand - The average grain size of sand particles - The clay content of the sand - The moisture level in the sand - Which equipment is used to test the fineness number of sand? - Sieve shaker - Permeability meter - Compression tester - Clay washer - Moisture content in green sand is: - 5-8% - 2-6% - 5-10% - 20-30% - Dry sand contain silica (SiO2) - 90-95% - 80-85% - 70-75% - 85-90% - Which instrument is used to determine the permeability number of molding sand? - Permeability meter - Sand sieve shaker - Compression tester - Clay washer | - The main purpose of a core in casting is_____________ - To improve the surface finish of the casting - To create hollow sections or cavities in the casting - To reduce the weight of the mold - To increase the melting point of the material - The common material used for making cores is _____________ in casting. - Wood - Green sand - Oil-bonded sand - Plastic - ____________is the primary binder used in core-making processes? - Sodium silicate - Water - Graphite - Bentonite clay - The property by virtue of which core ensures that it does not expand is ___________ . - Refractoriness - Permeability - Dimensional stability - Collapsibility - Core commonly used to create internal cavities in pipes is ____________. - Shell core - Horizontal core - Vertical core - Barrel core - Cracks in core are caused by________. - Excess binder - Rapid heating during baking - Uneven sand compaction - Excess moisture in the sand - Inaccuracies in mould cavity causes ______________. - Shrinkage - Warping - Misalignment - Gas porosity - In mould cope and drag are separated by _____________. - Gating system - Parting line - Core print - Vent holes - Pit molding is used to _____________. - Create small, intricate parts - Cast large, heavy components - Simplify mould assembly - Reduce material costs - The primary binder used in the CO₂ moulding process is ___________. - Bentonite - Sodium silicate - Resin - Clay - What is the role of CO₂ gas in this process? - To compact the sand - To harden the sodium silicate binder - To release gases from the mould - To prevent misalignment - Three piece pattern in CO2 moulding procees is used to: - Faster production time - To create complex castings with high precision - Lower cost of materials - Reduced risk of porosity defects - Poor bedding in pit moulding causes: - Cold shut - Core displacement - Misalignment - Gas porosity - To harden the core and remove moisture we perform: - Hammering - Baking - Pressing - machining - To allow escapes of gases in casting ________ are made in cores. - Bedding - Holes - Cracks - vents - In cold box core-making process___________ is used to harden the sand-binder mixture? - Heat - Carbon dioxide gas - Chemical catalysts - Steam - Mould dimensions are measured to check __________ of mold cavity - Design - Accuracy - Strength - None of these - ..................................is an advantage of using the CO₂ process? a) Reusability of sand b) High surface finish c) Rapid hardening of moulds d) Simplified mould removal | - To check the temprature of molten metal in casting ___________ is used. - Thermometer - Thermal gauge - Pyrometer - Multimeter - The range of temperatures optical pyrometer can measure is _________ - 0–500°C - 600–4000°C - 3000–6000°C - Below 0°C - To melt ferrous metals especially cast irom in casting ____________ furnace is used. - Blast furnace - Bessemer furnace - Muffle Furnace - Cupola Furnace - In cupola furncae ________ is used as fuel. - Coke - Wood - Natural gas - Charcoal - To protect cupola furnace shell from high temperatures_______________ material is used. - Composite - Polymer - refractory - fiber - To remove impurities in a cupola furnace ___________ is added. - Flux - Scrap metal - Alloying elements - Refractory material - In cupola furnace operation tapping process is used to___________ - Add scrap metal - Measure temperature - Remove molten metal - Insert the charge - To remove dissolved gases in non-ferrous casting __________ is uesd. - Flux - Degassing agents - Alloying elements - Refractory materials - Gas traped in casting casuses______________ - Cold shut - Porosity - Shrinkage cavity - Warpage - Premature solidification of metals in casusting causes___________. - Misrun - Blowholes - Hot tears - Slag inclusion - To ensure smooth finish after grinding ___________is performed. - Polishing - Heat treatment - Sand blasting - Surface coating - Tumling barrel machine in casting is used to_________________. - Remove excess material using heat - Clean and smooth casting surfaces through abrasion - Inspect casting defects - Alter the dimensions of the casting - The common method to inspect casting defects is____________. - Magnetic particle testing - Visual inspection - Ultrasonic testing - Radiography - Which of the following is NOT a surface treatment process. - Electroplating - Galvanizing - Tumbling - Painting - For non-ferrous components _____________ casting process is commonly used. - Sand casting - Investment casting - Shell molding - Die casting - ......................... is commonly used to clean castings and remove sand residues a) Shot blasting b) Grinding c) Annealing d) Heat treatment - Burned-on sand is typically removed using ...................... method. a) Sandblasting b) Grinding c) Ultrasonic cleaning d) Hand brushing - ........................... tools is used for grinding castings? a) Angle grinder b) Belt sander c) Die grinder d) All of the above - Tumbling is best suited for.............. a) Large and heavy castings b) Small and intricate castings c) Heat-resistant castings d) Welded components - The purpose of applying surface treatments to castings is to......... a) Enhance corrosion resistance and aesthetics b) Improve casting strength c) Remove internal defects d) Reduce production costs |

- Limited Response Questions

| Formative Assessment (Part A) | Formative Assessment (Part B) | Formative Assessment (Part C) |
| --- | --- | --- |
| LU 1 | LU 2-3 | LU 4-5 |
| Q1. Name the device use to measure moisture content in green sand. Q2. Name the defect caused by high moisture content in moulding sand. Q3. What does the permeability number of molding sand indicate? Q4. Write the effect of low permeability of sand on casting. Q5.Write down advantage of high green compressive strength of mould sand. Q6. Write down green sand composition. Q7. Wite down composition of dry sand. Q8. Enlist different types of sands used in casting. Q9. Write down three characteristcs of foundry sand. Q10. What is difference between facing sand and parting sand. | Q1. Enlist different types of cores used in casting. Q2. Write the purpose of baking core in casting. Q3. Write 03 characteristics of good core. Q4. Write names of differnt pattern types used in casting. Q5. Write names of different parts of mould. Q6. Write names of 05 different tools used in foundry shop. Q7. What is the purpose of using core in casting? Q8. Define pit moulding. Q9. Define CO2 Moldin techniques. Q10. What is the purpose of bedding in pit molding. | Q1. Write names of different steps of casting process. Q2. Define melting point of metals. Q3. Write melting point of cast iron, steel and aluminum. Q4. Write safety precautions in pouring molten metals. Q5. Enlist parts of cupola furnace. Q6. Write name of different casting defects. Q7. Write remedy to contol blow hole in casting. Q8. Write name of tools used for grinding casting products. Q9. Write names of different furnaces used in casting. Q10. Write 05 remedies to prevent defects in casting. |

- Assessment Tasks

| Formative Assessment (Part A) | Formative Assessment (Part B) | Formative Assessment (Part C) |
| --- | --- | --- |
| Prepare fine green sand for mold, check its composition, moisture content and compressive strength. Performance Criteria : - Apply safety protocol - Adapt Green Practices - Identify the tools and material - Select the mateials(silica sand, clay,water) - Mix the material - Check Composition of the Green Sand (sand content, clay content) - Measure the composition of moister content - Conduct compressive strentgh test to check compressive strength | Prepare a pit mold with bedding technique for two piece wooden pattern with round core. OR Prepare a Two-Piece Mold Using Pit Molding method Performance Criteria : - Apply safety protocol - Adapt Green Practices - Select the relevant tools and two-piece wooden pattern - Prepare green sand with the correct composition - Prepare drag (putting and pressing sand in it using relevant tools) - Place two-piece wooden pattern and round core in the drag part of moulding box in correct position - Place cope on it - Clamp cope and drag firmly - Put and presss the sand in drag portion of the moulding box - Make runner , riser and venting in the drag portion of moulding box using relevant tools - Seperate cope and drag - Remove the two piece wooden pattern using relevant tool - Clean the mould surface - Dry the mould - Inspect and check the mould | Perform casting of the given object, finish the object to required specification by grinding and tumbling barrel machine and inspect the finished part for casting defects. Performance Criteria : - Apply safety protocol - Adapt Green Practices - Identify the tools , materials - Collect the tools - Ensure the mould of given part is cleen and dry - Melt the material (Costiron or Aluminum) in crucible in the furnace upto the desired teperature - Pour the molten metal through spru in the mould cavity - Allow the molten metal to cool and get solidify - Break the mould safely and remove the casted material - Grind the casted mateial to the required specification - Place the casted material in a tumbling barrel machine. - Operate the machine as per the specified duration and speed to achieve the desired surface finish - Inspect the Finished Part for visible defectes such as crackes - Check the Dimensional Accuracy of the finished part using appropriate tools (e.g., calipers or micrometers) to ensure compliance with specifications. - Identify internal or hidden defects using appropriate methods (e.g., dye penetration, ultrasonic testing, or radiography) if the said testing fascility is available. |